| DATA SHEET: Melamine Doors – Core expanded polystyrene |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Leaf Construction | Door type | Interior door: sliding or swing. |  |  |  |  |  |  |  |  |  |  |
|  | Interior Door Frame | Spruce pine section 30x25mm (in 35mm door) |  |  |  |  |  |  |  |  |  |  |
|  | Door Core | Expanded polystyrene 27/30 kg/m3 Density |  |  |  |  |  |  |  |  |  |  |
|  | Facing | Medium density fibreboard (650-700 kg/m3) on 5/7mm thick. Finished on decorative melamine. |  |  |  |  |  |  |  |  |  |  |
|  | Facing Properties | Density |  | EN ISO 1183-1 |  |  |  |  | Density g/cm3 (mín.) 1,35 |  |  |  |
|  |  | Abrasion resistance |  | EN 438-2:10 |  |  |  |  | Revolutions (mín.) 150 |  |  |  |
|  |  | Impact resistance |  | EN 438-2:20 |  |  |  |  | Spring strength , N (mín.) 20 |  |  |  |
|  |  | Scratch resistance |  | EN 438-2:25 |  |  |  |  | strength (mín.) 2/3 |  |  |  |
|  |  | Stain resistance |  | EN 438-2:26 |  |  |  |  | Appearance , index (mín.) 5/4 |  |  |  |
|  | CANTO | PVC 0,8mm thickness ( Variable thickness depending on finish ) |  |  |  |  |  |  |  |  |  |  |
| Exterior door Frame | Jamb Material (on demand) | Waterproof or standard mdf according to requirements . Density 650-700kg/m3 |  |  |  |  |  |  |  |  |  |  |
|  | Jamb Finish (on demand) | Foil finish similar to leaf finish |  |  |  |  |  |  |  |  |  |  |
|  | Casing material (on demand) | Waterproof or standard mdf according to requirements . Density 650-700kg/m3 |  |  |  |  |  |  |  |  |  |  |
|  | Casing finish (on demand) | Foil finish similar to leaf finish |  |  |  |  |  |  |  |  |  |  |
|  | Jamb and Casing Core propereties (for water resistance material) | Humidity |  |  | EN 322 |  |  |  |  |  | 4%-11% |  |
|  |  | Tolerance in density |  |  | EN 323 |  |  |  |  |  | ±7% |  |
|  |  | Formaldehyde content |  |  | EN 120 |  |  |  |  |  | E1 ≤ 8mg/100g |  |
|  |  |  |  |  |  |  |  |  |  |  | E2 ≤ 30mg/100g |  |
| Leaf | Dimensional tolerances S/UNE EN 1529 | Squareness | ±1,5mm |  |  |  |  |  |  |  |  | (clase 1) |
|  |  | Height and width | ± 2mm |  |  |  |  |  |  |  |  | (clase 1) |
|  |  | Thickness | ±1,5mm |  |  |  |  |  |  |  |  | (clase 1) |
|  | Flatness S/UNE EN 1530 | Praise | ≤4mm |  |  |  |  |  |  |  |  | (clase 3) |
|  |  | curvature of longitudinal beams | ≤4mm |  |  |  |  |  |  |  |  | (clase 3) |
|  |  | curvature headwalls | ≤2mm |  |  |  |  |  |  |  |  | (clase 3) |
|  |  | local flatness | ≤0,3mm |  |  |  |  |  |  |  |  | (clase 3) |
|  | Hard Body Shock S/UNE EN 1192 | Maximum diameter (20mm) |  |  |  |  |  | Result: 9mm |  |  |  |  |
|  |  | Average depth of footprint (≤1mm) |  |  |  |  |  | Result: 0,1mm |  |  |  |  |
|  |  | Maximum depth of footprint |  |  |  |  |  | ≤1,5mm |  |  |  |  |
|  | Soft and heavy body shock resistance | No breakage or delamination. |  |  |  |  |  |  |  |  |  |  |
|  | Inmersion in water S/UNE 56 803 | Swelling |  |  |  |  | 1,4% |  |  |  |  |  |
|  |  | Remarks |  |  |  |  | No delamination |  |  |  |  |  |
|  | Screw removal S/UNE 56 803 | Average value (≥500N) |  |  |  | Results |  |  |  | Faces: 1034N |  |  |
|  |  | Minimun value (≥500N) |  |  |  |  |  |  |  | Edges: 1189N |  |  |

* See detail of the sheet on the next page

DATA SHEET: Melamine Doors – Core expanded polystyrene

Signed:

Jesús Bejo Santiago

Quality Manager